# Lime Plaster Technology — Sustainable Building Systems

(SpecX Knowledge Hub — Sustainable Materials & Heritage Practices)

## 1. Overview

Lime plaster is a traditional yet scientifically relevant building material used for sustainable architecture and heritage conservation. Composed primarily of natural hydraulic lime (NHL), aggregates, and pozzolans, it hardens through hydration and carbonation, forming a breathable and flexible matrix.

## 2. Composition & Material Science

| Component | Function | Notes / Standards |
| --- | --- | --- |
| Natural Hydraulic Lime (NHL 2–3.5) | Primary binder — hardens through hydration and carbonation | Defined under EN 459-1 |
| Pozzolanic Additives | Enhance strength & sulfate resistance | Volcanic ash, natural pozzolans, calcined clays |
| Aggregates (Dolomitic / Siliceous Sands) | Control shrinkage & porosity | Rounded river sands preferred |
| Marble Dust / Inert Fillers | Improve smoothness & finish | Common in finishing coats |
| Natural Organic Modifiers | Enhance workability & flexibility | Casein, cellulose, starch, plant resins |

## 3. Layer System — Generic Application Sequence

1. Surface Preparation — remove cement renders, efflorescence
2. Masonry Repair — fill joints & damaged areas with lime mortar
3. Bond Coat — improves adhesion, balances absorption
4. Base Plaster — main coat for levelling & moisture buffering
5. Dehumidifying Layer — open-pore layer for salt management
6. Finish Coat — smooth or textured lime finish
7. Breathable Paint / Limewash — final surface protection

## 4. Key Physical & Environmental Properties

| Property | Typical Range | Why It Matters |
| --- | --- | --- |
| Vapour Resistance (μ) | 3–6 | Enables evaporation, prevents condensation |
| Porosity | ≥ 40 % | Traps salts and maintains breathability |
| Thermal Conductivity (λ) | 0.3–0.5 W/m·K | Thermal buffer for stable interiors |
| Capillary Absorption | ≤ 0.3 kg/m²·h⁰·⁵ | Limits liquid water penetration |
| Compressive Strength | 1.5–5 MPa | Compatible with soft masonry |

## 5. Testing & Quality Standards

• EN 459-1 — Building Lime Specification
• EN 998-1/2 — Mortars for plastering and masonry
• WTA 2-9-04/D — Restoration plaster systems
• ISO 846 — Microbial Resistance Testing
• ASTM C270 / C28 — Mortar Specification for Masonry
• ICCROM / Getty — Conservation Guidelines